Comparison of Self Heating Effect between SOI and SOSiC MOSFETs

JM. Li1,2,3*, FY. Liu1,3, B. Li1,3, JJ. Li1,2,3, XG. Yao1,3, BG. Sun1,3, Y. Huang1,2,3, J. Wan4, Y. Xu5, S. Cristoloveanu6

1Institute of Microelectronics, Chinese Academy of Sciences, 100029 Beijing, China

2University of Chinese Academy of Sciences, Beijing 100029, China

3Key Laboratory of Science and Technology on Silicon Devices, Chinese Academy of Sciences

4State key lab of ASIC and System, Fudan University, Shanghai 200433, China

5College of Integrated Circuit Science and Engineering, Nanjing University of Posts and Telecommunication, Nanjing 210023, China

6GIICS, Guangzhou 510535, China

The requirements for electronic devices to withstand high temperatures have expanded, especially in sectors like oil exploration, aeronautics and automotive. Silicon-On-Insulator (SOI) MOSFETs are preferred for their fast switching and low leakage, showing superior high-temperature stability. However, they face self heating effect (SHE) due to poor heat dissipation through the buried oxide (BOX) [1]. SiC, with excellent thermal conductivity, is a better alternative to replace the BOX [2]. Using Si-on-SiC (SOSiC) substrates greatly improves the heat dissipation, reducing performance degradation due to SHE [3].

In this paper, we fabricated prototype SOSiC wafers by hydrophobic surface activation bonding (SAB) and analyzed the SHE of SOI and SOSiC MOSFETs using the calibrated TCAD simulations (Fig. 1). Their electrothermal properties, temperature rise, and thermal resistance are addressed. Furthermore, we investigated the heat dissipation paths of SOI and SOSiC MOSFETs, and elucidated the impact of the geometrical configuration of the devices on the relationship between temperature rise, thermal resistance, and dissipation pathways.

Fig. 2 shows that SOI MOSFETs suffer more serious on-state current degradation than SOSiC. At room temperature, the hot-spots are 347 K for SOI and 310 K for SOSiC, located near the LDD boundary due to uneven heat distribution (Fig. 3). The temperature rise and thermal resistance of the SOI MOSFETs are 3.9 and 4.1 times higher than those of SOSiC MOSFETs, which are more efficient in reducing junction temperature at same power levels. The comparison of the heat flux ratios across thermal contacts shows that SOI MOSFETs primarily dissipate heat through the drain and source (33.7% and 32.9%), while the substrate is the main heat path for SOSiC (85.6%), see Fig. 4 and 5.

As the epilayer thickness increases from 0.1 μm to 0.3 μm, the temperature rises in SOI by 52.4% despite the thermal resistance decreases by 1.8% (Fig. 6), which indicates that the increased current in thicker layers has a greater effect on SHE than the reduction in thermal resistance. For SOSiC, the temperature rise also increases for thicker layers but is limited to 15 K (Fig. 6). Meanwhile, heat dissipation through the source, drain, gate, and substrate indicates a correlation between dissipation paths and epilayer thickness (Fig. 6).

References

[1]	A. K. Goel and T. H. Tan, Microelec. Eng. 37 (2006) 963-975.

[2] 	T. Y. Li, Microelec. Eng. 46 (2016) 685-689.

[3] 	H. Shinohara, H. Kinoshita, M. Yoshimoto, Appl. Phys. Lett. Eng. 93 (2008) 122110.

Fig. 1. (a) Photograph and TEM image of SOSiC wafer.  (b) Structure of SOI and SOSiC MOSFET.

Fig. 2. (a) Calibration of SOI with experimental data.  (b) The Transfer and output characteristic curves of SOI and SOSiC with and without the SHE considered.

Fig. 3. (a) Lattice temperature distribution and the hotspot. (b) Temperature distribution in horizontal and vertical directions.

Fig. 4. Comparison of lattice temperature rise and thermal resistance between SOI and SOSiC.

Fig. 5. Main heat dissipation paths and heat flux ratios across thermal contacts.

Fig. 6. Variation of the temperature rise, thermal resistance and heat flux width of SOI and SOSiC as Hepi increases from 0.1 μm to 0.3 μm.

* Corresponding author: email: liufanyu@ime.ac.cn (FY. Liu), libo3@ime.ac.cn (B. Li)