Investigation of DC and Low Frequency Noise Parameters of Junctionless GAA Si VNW pMOSFETs in the Temperature Range from 80 K to 340 K

A. Tahiat1, B. Cretu1, A. Veloso2, E. Simoen2,3

1Normandie Univ, ENSICAEN, UNICAEN, CNRS, GREYC, 14000 Caen, France

2Imec Kapeldreef 75 B-3001 Leuven, Belgium

3Solid-State Sciences Department, Ghent University, 9000 Gent, Belgium

In this article, junctionless vertical nanowire (JL VNW) Gate-all-around (GAA) silicon field-effect transistors (FETs) manufactured at imec have been studied, in a wide range of temperature from 340 K down to 80 K, by performing direct current (DC) and low-frequency noise (LFN) measurements. The aim of this experimental study is to investigate the temperature dependence of the extracted DC parameters (low field mobility (µ0), threshold voltage (Vth), access resistance (Raccess), subthreshold slope (SS) etc.), and LFN parameters (flicker (1/f) noise level, volume trap density Nit, etc.), for the studied devices in order to evaluate their performance. The investigated devices are silicon NWs with a diameter of ~18 nm and a length of ~56 nm, which have been epitaxially grown on Silicon-on-Insulator (SOI) substrate. They are B-doped, JL and asymmetric (RDrain ≠RSource) devices, more fabrication details can be found in [1]. Two different devices were tested, devices #1 have 20 by 20 NWs in parallel while devices #2 have 30 by 40 NWs resulting in total 400 NWs and 1200 NWs for device #1 and #2 respectively. The measurements were made in ohmic regime with a drain-source bias of |VDS| = 50 mV, in forward and reverse (F/R) operation mode. The experimental set-up and the parameters extraction methodology are described in [2,3]. According to the figures 1.a and 1.b (device #2, |ID,(F/R)| vs. -VG curves) an increase of leakage current in forward operation mode is observed, which may testify that, it suffers from the GIDL effect [4], due to the high doping concentration of the drain and/or the S/D asymmetry. From figure 1.c, a decrease in |ID,ON| for lower temperature (T), may be observed and no zero-temperature coefficient (ZTC) point was observed in the investigated temperature range. However, a better SS was perceived for lower temperatures until T = 120 K as illustrated in figure 2.a. In figure 2.b, Vth is negatively shifted with a slope of about -1.3 mV/K. A significant degradation of the low field mobility is noticed as the temperature decreases. It may be suggested that scattering by surface oxide charges may be the dominating mechanism causing µ0 degradation as can be observed in figure 2.c, since the evolution of the extracted µ0 is proportional to the temperature [5]. It is important to note that a decrease in the extracted Raccess, when the temperature decreases was also observed for both devices, see Figure 2.c (right). On the other hand, the LFN measurements reveal an increase in the input referred noise power spectral density (PSD) as the temperature decreases for the same |Vov|, (|VG-Vth|) as illustrated in figure 3.a. Figure 3.b shows the 1/f noise level vs. |Vov| for device #1. For T = 300 K, the dominant noise contributions are the correlated carrier number and mobility fluctuations mechanism (CMF + CNF), and the Raccess noise contribution at high |Vov| values, (no impact of the S/D asymmetry was observed on the LFN). For T = 150 K and 80 K only CMF + CNF was observed, which may be related to the decreasing of the Raccess. A correlation was fond between mobility µ0 degradation and the estimated flat-band noise level (Svfb) and Nit increasing as exposed in figure 3.c. This correlation suggests an impact of the charge oxide traps on both 1/f noise level and low filed mobility through remote Coulomb scattering.

References

E. Simoen, A. Veloso, Ph. Matagne, C. Claeys, “Impact of the channel doping on the low-frequency noise of gate-all-around silicon vertical nanowire pMOSFETs,” Solid-State Electronics, Vol. 200, 2023.

A. Tahiat, B. Cretu, A. Veloso, E. Simoen, “Novel Y-function based strategy for parameter extraction in S/D asymmetric architecture devices and low frequency noise characterization in GAA Si VNW pMOSFETs, Solid-State Electronics,” Vol. 209, 2023.

B. Cretu, A. Veloso and E. Simoen, “Refined DC and low-frequency noise characterization at room and cryogenic temperatures of vertically stacked silicon nanosheet FETs”, in IEEE Transactions on Electron Devices, vol. 70, no. 1, pp. 254-260, 2023.

G. Ghibaudo, “Critical MOSFETs operation for low voltage/low power IC's: Ideal characteristics, parameter extraction, electrical noise and RTS fluctuations,” Microelectronic Engineering, Vol. 39, Issues 1–4, p. 31-57, 1997.

Figure 2: (a) SS as a function of temperature for device #1 (left) and device #2 (right). (b) Threshold voltage Vth as a function of temperature with |VDS|= 50 mV. (c) Extracted low field mobility parameter µ0 (left) and access resistance Raccesss (right) vs. temperature for the studied devices.

Figure 1: Absolute drain current |ID| vs. - applied gate voltage in forward (a) and reverse (b) operation mode (in log scale) as a function of temperature for device #2 (1200 NWs). (c) Absolute drain current |ID| (in linear scale) vs. absolute gate voltage overdrive |VG-Vth| for device #1 (400 NWs) as a function of temperature.

C.T. Sah, T. H. Ning and L. L. Tschopp, “The scattering of electrons by surface oxide charge and by the lattice vibrations at the Si-SiO2 interface,” Surface Sci., vol. 32, p. 561-575, 1972.

Figure 3: (a) typical 1/f input-referred voltage noise PSD Svg vs. frequency for different temperatures at |Vov| ≈ 0.330 V and VDS = -50mV for device #1 and #2. (b) Input-referred 1/f noise level vs. the gate voltage overdrive (Vov), for temperatures T=300 K, 150 K and 80 K for device #1. (c) Estimated flat-band noise levels (left) and Nit (right) vs. the inverse of the extracted low field mobility for T = 300 K, 150 K and 80 K for device #1 and #2.

Corresponding author: email: Abderrahim.tahiat@ensicaen.fr