Novel Y-function methodology parameter estimation from weak to strong inversion operation

A. Tahiat1, B. Cretu1, A. Veloso2, E. Simoen2,3

1Normandie Univ, ENSICAEN, UNICAEN, CNRS, GREYC, 14000 Caen, France

2Imec Kapeldreef 75 B-3001 Leuven, Belgium

3Solid-State Sciences Department, Ghent University, 9000 Gent, Belgium

Considering the expressions of the drain current and of the transconductance in ohmic operation regime [1], and of the general assumed extrinsic effective mobility [2,3]:

ID=WLµeffQiVDS	(1) ;  gm=WVDSLCoxCiCox+Cd+Cit+Ci∂µeffQi∂Qi (2);  µeff=µ01+θ1QiCox+θ2QiCox2 (3)

the expression of the Y-function may be derived as:

Y=IDgm=GMVDS1-θ2QiCox2SSln10+QiCoxQiCox					(4)

where GM=Wµ0Cox/L [2]; W and L the effective width and length of the channel; µeff the extrinsic effective mobility; µ0 the low field mobility; θ1 and θ2 the first and second mobility attenuation factors; Qi the inversion charge density; VDS the drain to source voltage; Cox, Cd, Cit and Ci are the gate, depletion, interface state and inversion charge capacitances per unit or area and SS the subthreshold swing. Assuming that Ci≪Cox+Cd+Cit in weak inversion and Ci≫Cox+Cd+Cit in strong inversion with Ci=qQikBT (kBTq being the thermal voltage) [1] the QiCox may be evaluated: in weak inversion as: QiCox=Y2GMVDSSSln10 (5) and in strong inversion as QiCox=YGMVDS+θ2Y2  (6). Without any approximation, from weak to strong inversion the ratio QiCox may be expressed as: GMVDS+θ2Y2QiCox2+GMVDSSSln10QiCox-Y2=0 	(7).

The GM and θ2 parameters were extracted using criteria of [3] and the subthreshold swing SS may by determined from I-V curves in the subthreshold zone. Consequently, the QiCox ratio may be easily evaluated from weak to strong inversion operation by solving the second-degree equation of (7) (Figure 1). Further, the drain current may be evaluated using (1), having θ1 estimated using [3] and the transconductance using (2) or gm=ID2Y2, where Y is modeled using (3). Very good agreement between the experimental ID and the gm models of (1), respectively (2) may be observed for devices for different technologies (Figure 2 and 3), even at 80 K operation (Figure 3).

The advantage of this new methodology is that no capacitance measurements or mathematical formulation as Lambert W function or Kubo-Greenwood modeling approach are necessary [4,5]. Moreover, only four parameters are needed to be estimated: three extracted in strong inversion (GM, θ2 and θ1) and one estimated in the subthreshold zone (SS). The inversion charge over the gate capacitance ratio is estimated using its dependency on the Y-function described in (7). Finally, a compact Y-function methodology may be proposed, providing accurate and physical electrical parameters extraction and allowing to model the transfer characteristics behaviour from weak to strong inversion operation regime if the drain current may be expressed as in (1) and the extrinsic effective mobility as in (3).

References

G. Ghibaudo, “Analytical modelling of the MOS transistor”, Phys. Stat. Sol. (a), 113(1), p. 223-340, 1989.

C. Mourain, B. Cretu, G. Ghibaudo, and P. Cottin, “New method for parameter extraction in deep submicrometer MOSFETs”, IEEE 2000 Int. Conf. On Microelectronics Test Structure (ICMTS 2000), 181-186, 2000.

B. Cretu, A. Veloso, and E. Simoen, “Refined DC and low frequency noise characterization at room and cryogenic temperatures of vertically stacked silicon nanosheet FETs”, IEEE Trans. Electron Dev., 70(1), 254-260, 2023.

F. Serra di Santa Maria, L. Contamin, B. Cardoso Paz, M. Cassé, C. Theodorou, F. Balestra, G. Ghibaudo, “Lambert-W function-based parameter extraction for FDSOI MOSFETs down to deep cryogenic temperatures”, Solid-State Electron., 186 (12), pp. 108175, 2021.

Figure 2: ID vs. VGS in linear scale (a) and log-lin scale (b); (c) gm vs. VGS; Good agreement between the experimental (symbols) and the model (full line) is observed.

Figure 3: ID vs. VGS in linear scale (a) and log-lin scale (b); (c) gm vs. VGS, Good agreement between the experimental (symbols) and the model (full line) can be observed. circle points represent 300 K, square points represent 80 K temperature operation. GAA NS FET device: L / W = 100 nm / 2288 nm, EOT of 0.9 nm; vertical distance between the stacked nanosheets 7.5 nm.

Figure 1: (a) QiCox versus the applied gate voltage estimated from (5) (short-dot line), from (6) (short dash line) and from (7) (full line). (b) ∂logID∂VGS permitting the estimation of the SS parameter. (c) very good agreement between the experimental Y-function and model of (4). UTBOX n-channel device: L / W = 120 nm / 1 µm, EOT of 2.6 nm, after processing a BOX thickness TBOX of 15 nm and a silicon film thickness TSi of 16 nm.

F. Serra di Santa Maria, L. Contamin, M. Cassé, C. Theodorou, F. Balestra, G. Ghibaudo, “Comprehensive Kubo-Greenwood modelling of FDSOI MOS devices down to deep cryogenic temperatures”, Solid-State Electron., 192 (6), pp. 108271, 2022.

Corresponding author: email: bogdan.cretu@ensicaen.fr